## Slide 1: Graphene Devices for Beyond-CMOS Heterogeneous Integration
Mohamed Darwish

## Slide 2: What’s next on the Roadmap?
W. Arden, M. Brillouët, P. Cogez, M. Graef, B. Huizing, and R. Mahnkopf, “‘More-than-Moore’ White Paper.”
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 3: Beyond-CMOS, More Moore and More than Moore
IBM
S.-J. Han, A. V. Garcia, S. Oida, K. A. Jenkins, and W. Haensch, “Graphene radio frequency receiver integrated circuit,” Nat. Commun., vol. 5, pp. 1–6, Jan. 2014.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 4: New Architecture and Device Paradigms
Architecture
Quantum
Neuromorphic
Information Processing
Device-Aware Synthesizers
Stochastic Computing
Error-Prone Computing
Device
2D FET
CNT
Tunnel FET
Spintronic
GpnJ
Magnetic
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 5: We Need Paradigm Shifts
System Architecture
Module
Gate/Circuit
Device
System
Circuit
Device
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 6: What is graphene?
1 layer of graphite = graphene
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 7: Graphene’s Band Structure
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 8: Graphene’s dispersion relation – High Symmetry Points
Most device operate in this range
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 9: What’s special about the Dirac points?
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 10: Why graphene?
CVD growth allows wafer-scale coverage
CMOS Compatible
Unique electronic properties enabling novel devices beyond Transistors
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 11: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 12: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 13: Why Cellular Neural Network?
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Neural Networks have been very successful in classification and image processing problems
One circuit-friendly implementation (Cellular Neural Networks) have been around since the 1980s
CNN implementation are size limited
  Excessive power consumption limits the number of cells
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 14: Cellular Neural Networks - Architecture
4x4 CNN
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 15: Cellular Neural Networks – System Model
We have 3 parameters in a CNN: Input (): External Stimulus State (): Internal parameter Output (): Function of the state
The network is stable as long as the output is related to the state by a monotonic, bound function (sigmoid)
Synaptic weights control circuit function and are determined offline
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 16: Cellular Neural Networks – Neuron Circuit Model
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Input
Stimulus
State Variable
Output Sigmoid
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 17: CMOS implementation of Canonical CNN
Canonical CNN implementations is suitable for CMOS
  Several Analog implementations available
  Nonlinearity not a problem as long as its monotonic
Synaptic weights implemented using transconductors
  Need to be tunable with good matching
  Put a lower bound on the current consumption ()
  Number of Synapses >> Number of Neurons
Neuron RC controls system dynamics and speed
  Neuron C >> Parasitic Capacitance for reliable operation
  R not too big to reduce the noise in the system, but
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 18: Problems of CMOS CNN
Power Consumption
Dominated by Synapse Transconductors
Large number of Synapses
Matching and Tuning Requirements
Synapse Transconductance needs to be tunable
Synapses must be well matched
Speed Limitations
Neuron C >> Parasitics for Robustness
Lower RC means more power consumption
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 19: What can graphene do?
Graphene provides variable, finite channel resistance
  Voltage controlled resistor or low output resistance transistor
CVD graphene allow us to create high density of devices
Graphene is compatible with CMOS
  Allows leveraging the high memory density available in CMOS
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 20: Graphene Resistance vs Gate Voltage
CVD graphene operates typically in the diffusive regime (Drude Model)
One popular model is the constant mobility model
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 21: All-Graphene CNN - Architecture
Fixed total R >>
M. Darwish, V. Calayir, L. Pileggi, and J. A. Weldon, “Ultracompact Graphene Multigate Variable Resistor for Neuromorphic Computing,” IEEE Trans. Nanotechnol., vol. 15, no. 2, pp. 318–327, Mar. 2016.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 22: All-Graphene CNN – Architecture Properties
Neurons formed by a string of two voltage controlled resistors
  Inhibitory/Excitatory resistors pull towards ground/supply respectively
Neuron Capacitor stores the state
Synapses formed via two complementary digitally-controlled resistors
  Scales the output of the neuron before applying it to the inhibitory/excitatory control of the neighbor neuron
Both neurons and synapses formed via dual-gates graphene FETs
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 23: All-Graphene CNN – Architecture Properties
Pros
Implicit sigmoidal behavior.
Synapse power consumption can be made arbitrarily small.
Reduced parasitic capacitance at state variable node.
Synapse matching required locally not globally.
Cons
Neuron RC limits speed.
More complicated training.
Network size limited by gate strength.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 24: Constant Mobility Model
(Charge-Neutrality Point)
: Contact Resistance
: Back gate oxide areal capacitance
: Electronic charge
: Number of squares in the channel
S. Kim, J. Nah, I. Jo, D. Shahrjerdi, L. Colombo, Z. Yao, E. Tutuc, and S. K. Banerjee, “Realization of a high mobility dual-gated graphene field-effect transistor with Al2O3 dielectric,” Appl. Phys. Lett., vol. 94, no. 6, p. 62107, 2009.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 25: Neuron/Synapse: Device Structure
M. Darwish, V. Calayir, L. Pileggi, and J. A. Weldon, “Ultracompact Graphene Multigate Variable Resistor for Neuromorphic Computing,” IEEE Trans. Nanotechnol., vol. 15, no. 2, pp. 318–327, Mar. 2016.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 26: Notable Fabrication Details
Contacts cannot be sputtered to prevent damage to graphene
  Evaporation causes no kinetic impact damage unlike sputtering
Top gate oxide require a seed as non-functionalized ALD precursors do not react with the graphene surface and preferentially react with reactive graphene edges
Top gate oxide ALD relieves stress developed during contacting, etching and seed layer deposition (more on this later)
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 27: Neuron/Synapse: How they look like
3-bit Synapse
3-input Neuron
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 28: Interesting Synapse Behavior
VBG>VD
VBG<VD
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 29: Synapse as Dual-Slope Digital-to-Resistance Converter
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 30: Measured Synapse Resistance Change
Expected
Measured
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 31: Synapses as Digital-to-Resistance Converter
Synapses act as Digital-to-Resistance Converter
Slope and magnitude of resistance change controlled by back gate voltage
Process variability reduced using CMOS-like techniques (ex. Common centroid)
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 32: System-Level VerilogA Simulation
VerilogA models developed based on measurement results
Classification trained using Hebbian learning offline and successful up to 28% distortion
System can also perform edge and line detection
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 33: Conclusion
System-Circuit-Device co-design enable multi-level innovations
New architecture relaxes chip-level matching constraints
Graphene enables area-efficient implementation of synapses and neurons
Graphene synapses are compact digital-to-resistance converters
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 34: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 35: A review of graphene diodes
Linear dispersion and continuum of states except at the Dirac point make graphene diodes attractive
  Lossless as there is no barrier potential
  Relies on optics-inspired techniques for conduction anisotropy
Can be used for low-loss scavenging of RF power or diode-based mux logic
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 36: Mux Logic
S. Miryala et al., “Delay model for reconfigurable logic gates based on graphene PN-junctions,” in Proceedings of the 23rd ACM international conference on Great lakes symposium on VLSI - GLSVLSI ’13, 2013, vol. 2, no. 1, p. 227.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 37: Geometric Graphene Diodes
Geometric diodes proposed to achieve asymmetric conduction by collimation of charge carriers in one direction and not the other
Fabricated using exfoliated and CVD graphene
  Exfoliated graphene devices always had higher asymmetry
  Hints to the role of scattering
Maximum achieved asymmetry was ~1.37 using exfoliated graphene
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 38: Principle of operation of geometric diodes
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 39: Oblique Incidence Graphene Diodes
Graphene charge carriers follow a Snell’s-law like relation at interfaces
Total internal reflection of charge carriers at oblique interfaces if angles, doping and Fermi level set correctly
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 40: Proposed Oblique Incidence diode
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 41: Interface Transmission Asymmetry
Left-to-Right
Right-to-Right
E1 = 0.5 eV, E2 =-0.5eV
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 42: Oblique PN junction model
Scattering smears the angular distribution and limits the backward-to-forward resistance ratio
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 43: Measurement Results
A = I(VFWD)/I(VBWD)
Highest Graphene Diode Asymmetry reported to date!
Best reported Geometric Diode
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 44: Conclusion
Geometric diodes show that exfoliated graphene is better than CVD graphene
Measurements show that CVD oblique incidence diodes outperform exfoliated geometric diodes
Asymmetry is still too low for practical devices
  Scattering and lead resistance need to be reduced
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 45: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 46: Graphene Coupler
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 47: Why study resistive coupling?
Ballistic-transport devices predicted to have periodic coupling coefficient like their optics counterparts
Diffusive-transport couplers never studied
  Could they be useful?
  How does diffusive transport affect the coupling coefficient?
Capacitive coupling and cross-talk have been thoroughly investigated, but no study of scaling limits in terms of resistive coupling
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 48: Electrical model of diffusive coupler
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 49: Electrical model details
Loss of phase information by scattering allows us to model coupling using a resistance
Sheet resistance of each branch assumed to be the same for simplicity
  Process gradient can be assumed negligible if ribbons are not too far apart
  Charge-puddles average out macroscopically
Coupling conductance per unit length obtained via Bardeen Transfer Hamiltonian (BTH)
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 50: Is this model accurate?
Loss of phase information preserved
All distributed resistances should be random variables
Can be relaxed to first order models and when ribbon spacing is too wide relative to LER
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 51: SPICE simulation results
,
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 52: Coupling conductance estimation
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 53: Coupling conductance results
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 54: Conclusion
Diffusive-transport couplers have an asymptotic coupling coefficient
  Not periodic like ballistic-transport couplers
Resistive coupling not a concern for deeply scaled graphene ribbons
Coupling conductance is negligible for ligthographically-defined ribbons
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 55: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 56: Impact of Metal-Graphene Interface on Device Performance
Joule heating increases channel temperature increasing scattering and reducing mobility
Proper device design enhances graphene-metal thermal contact allowing heat to escape through the contact reducing the channel heating
Thermal contact optimization should not affect electrical contact resistance to prevent reduction in electrical device performance
D. Saha, X. Yu, M. Darwish, M. Jeong, J. Freedman, A. Gellman, J. Weldon and J. Malen, “Developing Superior Alloy Contacts Optimized for Electrical and Thermal Transport at Metal-Graphene Interfaces”, MRS Spring, April 2017
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 57: Contact Metal Choice
Ni and Pd are known to have the lowest electrical contact resistance to graphene
Compositionally Spread Alloy Film (CSAF) or Ni-Pd was evaporated on a blanket graphene film over 90 thermal SiO2 and graphene-metal interface thermal conductance (GTH) was evaluated FDTR (Frequency Dependent Thermal Reflectance)
  All sample covered with Au transducer layer
Higher thermal interface conductance is desirable as it means more heat can flow across the metal contact rather than through the channel
D. Saha, X. Yu, M. Darwish, M. Jeong, J. Freedman, A. Gellman, J. Weldon and J. Malen, “Developing Superior Alloy Contacts Optimized for Electrical and Thermal Transport at Metal-Graphene Interfaces”, MRS Spring, April 2017
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 58: FDTR setup
J. Epstein, W. L. Ong, C. J. Bettinger, and J. A. Malen, “Temperature Dependent Thermal Conductivity and Thermal Interface Resistance of Pentacene Thin Films with Varying Morphology,” ACS Appl. Mater. Interfaces, vol. 8, no. 29, pp. 19168–19174, 2016.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 59: Evaluated Metal-Graphene GTH
D. Saha, X. Yu, M. Darwish, M. Jeong, J. Freedman, A. Gellman, J. Weldon and J. Malen, “Developing Superior Alloy Contacts Optimized for Electrical and Thermal Transport at Metal-Graphene Interfaces”, MRS Spring, April 2017
Elemental metals lie in this range
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 60: Electrical Measurements
Currently another CSAF sample is being created with electrical and thermal measurements structures
  Electrical: Linear TLM, Circular TLM, CBKR and 4-point probe
  Thermal: Metal strips
Will the electrical contact resistance show the same trend?
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 61: Stress in GFETs
Contacts anchor the graphene to the substrate
Graphene is single-atom thick, surrounded by materials of different thermal expansion coefficient
  Highly prone to stress
α1
Top Gate Oxide
Silicon Substrate
Bottom Gate Oxide
Graphene
Contact
Contact
Adhesion
Adhesion
α2
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 62: Probing Stress in Graphene
2D Raman peak red shifts under tension
2D Peak FWHM function of both stress and charge fluctuations
2D peak splits under
  Function of orientation, polarization and strain magnitude
Tension
M. Mohr, J. Maultzsch, and C. Thomsen, “Splitting of the Raman 2D band of graphene subjected to strain,” Phys. Rev. B, vol. 82, no. 20, p. 201409, Nov. 2010.
Compression
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Left/Right on the scale is more intuitive in the discussion over graphs.
Mention the 2D shift being an overtone of the breathing mode increasing the wavelength and hence causing red shift

## Slide 63: Device Structure used in Strain Evaluation
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 64: Strain Evolution during GFET Fabrication
M. Darwish, D. Saha, J. Malen, and J. A. Weldon, “Processing-Induced Strain in Dual-Gated Graphene FETs”, in IEEE Nano, 2017.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 65: Impact of Developer Chemistry on Device Performance
Photoresist developer chemistry can contain Metal-Ions or be Metal-Ion Free
Choice of developer chemistry is dictated by process compatibility and developer properties
Impact of Metal-Ion Free (MIF) and Metal-Ion Containing (MIC) developers on device performance evaluated using the constant mobility model
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 66: Dirac Point Shift
MIC
N=25
MIC
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: The results for each developer are presented using box plots, Central marker for median, Box edges are 25 and 75 percentile edges, Whiskers extend to most extreme data points.

## Slide 67: Field-Effect Mobility and Charged-Impurity Concentration
MIC
N=25
MIC
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: The results for each developer are presented using box plots, Central marker for median, Box edges are 25 and 75 percentile edges, Whiskers extend to most extreme data points.

## Slide 68: Contact Resistance
MIC
N=25
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 69: Mobility and Charged-Impurity Concentration
The mobility and charged-impurity concentration are inversely proportional
The relation between and is given as:
The value of the proportionality constant has been evaluated theoretically to be
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 70: Mobility vs Charged-Impurity Concentration
M. Darwish, D. Saha, J. Malen, and J. A. Weldon, “A Comparison of the Impact of Metal - Ion Containing and Metal - Ion Free Photoresist Developers on Graphene Field - Effect Transistors,” in IEEE Nano, 2017.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 71: What’s next?
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 72: Future Work – Contact Engineering
Co-optimization of electrical and thermal interface contact resistance by alloying can significantly enhance device performance
  CSAF films allow rapid evaluation and fine-tuning of contact alloys
Impact of adhesion layer evaluated using partial-coverage films
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 73: Future Work – Graphene leads for 2D materials
2D materials are doped by contacts
Integration of different metals for different device doping type is limiting, if possible
Graphene can act as an intermediate lead between the metal and 2D semiconductor to alleviate contact doping
  Can be combined with alloyed metal-graphene contacts
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 74: Future Work – Oblique diodes using hBN/G/hBN heterostructure
Exfoliated graphene between hBN flakes has low scattering
  Mean free paths (MFP) for up to a micron at room temperature
Oblique-incidence diodes fabricated using hBN/G/hBN heterostructure will have reduced scattering and higher asymmetry
The use of edge contacts allows reducing the parasitic contact resistance considerably
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 75: Future Work – CVD hBN with CVD graphene
hBN is the optimal substrate for graphene
Combining CVD hBN with CVD graphene enables wafer-level integration of high performance graphene devices
CVD of hBN has been demonstrated, but transfer along with CVD graphene is yet to be explored
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 76: Acknowledgements (1)
Prof. Jeffrey A. Weldon.
Prof. Larry Pileggi
Prof. Randall Feenstra
Prof. Eric Pop (Stanford University)

## Slide 77: Acknowledgements (1)
Prof. Andrew Gellman
Prof. Jonathan Malen
Prof. Ben Hunt
Prof. Tzahi Cohen-Karni

## Slide 78: Acknowledgments (2)
Dr. Mohamed Abdelmoula
Dr. Doron Naveh
Dr. Mathew Moneck
Nanofab Staff: Mark Weiler, Norman Gottron, Mason Risley, James Rosvanis
Ex. Nanofab Staff: Carsen Kline and Chris Bowman

## Slide 79: Acknowledgments (3)
Prof. Jelena Kovačević
Dipanjan Saha
Ning Wang (Stanford University)
Dr. Sergio de la Barrera
Devashish Goplan
Xiaoxiao Yu

## Slide 80: Acknowledgments (4)
David Bromberg, Tom Jackson, Jeff Zayas, Sean Yen, Omer Ozdemir, Yunlu Li, Isen Ozalp, Yunus Kesim, Sungho Kim, Nail Etkin “LL” Can Akkaya, Burac Erbagci, Luca Colombo, Mats Forssell, MaryBeth Galanko, Ashwati Krishnan, Metin Guney, Andrew Ong, Cheng-Ming Chow, Ekin Sumbul, Ahmed Abdelgawad, Usama Zaghloul, Ahmed Khairi, Ahmed Hussein, Mazen Soliman, Mohamed Mahmoud, Khaled El-Galaind, Ahmed Hefny and Waleed Ammar
Dr. Amani Attia
Dr. Ashraf Taha
This work was supported in part by Systems on Nanoscale Information fabriCs (SONIC), one of the six SRC STARnet Centers, sponsored by MARCO and DARPA

## Slide 81: Acknowledgments (5)
My Father, Omar Abdulaziz
My Mother, Mariam
My Sister, Mennatullah
My Son, Bilal
My Wife and support, Mai

## Slide 82: Questions?

## Slide 83: Fabrication Steps (1): Contact photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Positive photoresist (S1805) and lift-off layer (LOR3A) spin and bake
(b) Exposure and development in CD26 (TMAH-based MIF developer prevents graphene doping)

## Slide 84: Fabrication Steps (1): Contact photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties

## Slide 85: Fabrication Steps (2): Contact deposition and lift-off
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Evaporation of contact metal stack (Ti/Pd 1.5/40 nm at a rate < 0.3 Å/sec)
(b) Lift-off in a dedicated Microposit 1165 remover at 70 °C to prevent contamination

## Slide 86: Fabrication Steps (2): Contact deposition and lift-off
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties

## Slide 87: Fabrication Steps (3): Channel Etch Mask Photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Positive photoresist (S1805) and lift-off layer (LOR3A) spin and bake
(b) Exposure and development in CD26 (TMAH-based MIF developer prevents graphene doping)

## Slide 88: Fabrication Steps (4): Channel Definition using RIE
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Etch the exposed graphene in O2 plasma (20 W for 1 minute at 10 mTorr)
(b) Etch mask removal in a dedicated Microposit 1165 remover at 70 °C to prevent contamination

## Slide 89: Fabrication Steps (3): Channel Etch Mask Photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties

## Slide 90: Fabrication Steps (5): Top oxide seed layer and oxide deposition
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Evaporation of 1.5 nm of Al to act as a seed layer for ALD as non-functionalized ALD reacts only with graphene edges. 1.5 nm of Al are fully oxidized in air (Native Al oxide is 2.5 nm thick)
(b) ALD of Al2O3 at 150 °C to finish the top gate oxide deposition

## Slide 91: Fabrication Steps (6): Top gate e-beam lithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Positive e-beam resist (PMMA A7) and spin and bake beyond glass transition temperature
(b) Exposure and development (1:3 MIBK:IPA developer) of top gate electrodes

## Slide 92: Fabrication Steps (7): Top gate deposition
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Evaporation of top gate metal
(b) Lift-off of top gate metal in a dedicated acetone bath

## Slide 93: Fabrication Steps (7): Top gate deposition