## Slide 1: Graphene Devices for Beyond-CMOS Heterogeneous Integration
Mohamed Darwish
Notes: Good morning everyone. Mention name and Advisor. Welcome to my PhD Defense.

## Slide 2: What’s next on the Roadmap?
W. Arden, M. Brillouët, P. Cogez, M. Graef, B. Huizing, and R. Mahnkopf, “‘More-than-Moore’ White Paper.”
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Since its early days, the semiconductor industry’s economics relied on reducing the cost per function on chip, while fixing the cost per unit chip area, reducing the overall cost per function and allowing the integration of more functions for the same cost. This methodology paved the way for the versatile use of electronic components and moving them from a nice, high-end, low-volume market to high-volume consumer electronics. Historically, the reduction in cost per function was done by using clever circuit techniques and reducing the size of electronic components (scaling), which is what we know now as Moore’s law. The scaling trend is what we call now More Moore.
As the economic revenues of scaling started to wind down due to the increasing cost of new manufacturing tools, masks and the adverse impact of scaling on device performance, new techniques have been proposed to get over the scaling obstacles. In that sense, two more techniques were proposed to continue the reduction of cost per chip-integrated function: More-than-Moore and Beyond-CMOS.
Moore-than-Moore focuses on the integration of more circuit components on-chip, such as Analog circuits, Sensors and MEMS. Beyond-CMOS focuses on the integration of new materials with Silicon, the current workhorse material of the electronics industry, such as SiGe, III-V Semiconductors and 2D materials. In this work, we focus on the use of graphene with Silicon, or in other words, using graphene for beyond-CMOS heterogeneous integration,.

## Slide 3: Beyond-CMOS, More Moore and More than Moore
IBM
S.-J. Han, A. V. Garcia, S. Oida, K. A. Jenkins, and W. Haensch, “Graphene radio frequency receiver integrated circuit,” Nat. Commun., vol. 5, pp. 1–6, Jan. 2014.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Examples of all these trends can be found in the work published recently. The figure on the left shows the integration of inductors and capacitors on chip (Moore-than-More), with graphene channel transistors (beyond-CMOS), demonstrating the first functional graphene radio.
An example on More-Moore, is the 5 nm, GAA Silicon Nanoribbon transistors, which uses silicon nanoribbons surrounded by gates from all the directions to enable the fabrication of deeply scaled silicon transistors down to 5 nm.

## Slide 4: New Architecture and Device Paradigms
Architecture
Quantum
Neuromorphic
Information Processing
Device-Aware Synthesizers
Stochastic Computing
Error-Prone Computing
Device
2D FET
CNT
Tunnel FET
Spintronic
GpnJ
Magnetic
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: An aspect that people usually overlook when discussing scaling is the impact of clever circuit architectures and techniques in reducing the overall cost per function. Now, people have been looking back at that, investigating the different architecture-circuit-device co-optimization and design, to enable the integration of more area and power efficient functions, allowing us to reduce the overall cost and power-budget per function; an aspect crucial in today’s mobile and IOT-focused market.
An example of the new architecture trends is the use of brain-inspired or neuromorphic computing, quantum computing and error-prone computing to name a few.
In addition, new device architectures as 2D FETs, Tunnel FET and magnetic logic circuits are investigated as alternatives and additions to CMOS to allow further reduction in cost per function. However, these new design paradigms have been living in vacuum, without much collaboration, which has been the essence in top-down and bottom-up design approaches, that allow different levels of design abstraction to work independently.

## Slide 5: We Need Paradigm Shifts
System Architecture
Module
Gate/Circuit
Device
System
Circuit
Device
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: In this work, we show how a departure from the independent design abstraction paradigms into a collaborative device-circuit-system co-design allows us to fully-leverage the advantages of new materials. In this work, we will focus on the use of graphene in a non-transistor-centric way. We will focus on integrating functions into devices, where a device is designed to implement a high-level function, allowing considerable area and power savings.

## Slide 6: What is graphene?
1 layer of graphite = graphene
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Graphene is a single layer of carbon. For example, if you scribe a line with a pencil, this pencil line is made out of a graphite, which is composed of a huge number of graphene layers stacked all over each other. Each single layer of graphite is known as graphene.
The carbon atoms in graphene are placed in a hexagonal lattice as shown in the figure on the right. This lattice can be reconstructed using a two-atom unit cell using the two basis vectors shown. This peculiar placement of atoms gives graphene lots of unique properties.

## Slide 7: Graphene’s Band Structure
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Graphene’s electronic band structure has a hexagonal the Brillouin zone. The valence and conduction bands touch at vertices of the Brillouin zone hexagon corners. As such, graphene is a zero band-gap material, and is classified as a semimetal.

## Slide 8: Graphene’s dispersion relation – High Symmetry Points
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Most device operate in this range
Notes: In addition to the 6 fold hexagonal symmetry, the graphene band structure has mirror symmetric around the normal to the Brillouin zone edges. As such, we can reconstruct the information in the Brillouin zone using the area defined by the high symmetry points ΓMK. The band structure along the high-symmetry point shows that the band structures touch at the corners, which are known as the Dirac points, where most electronic device operate (most devices operate around a Fermi energy of 1 eV from the zero band-gap).

## Slide 9: What’s special about the Dirac points?
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Interestingly, the band structure looks conical around the Dirac point, resembling the energy dispersion of relativistic massless particles (photons), with the positive and negative energy particles (or electrons and holes) having the same mass. This gives rise to the very interesting physics, as it means that charge carriers act like photons in this regime. They follow a Snell’s law like at interfaces between regions of different doping and move around with a fixed velocity (Fermi velocity). A point to note however, that the Dirac points are not all equivalent; any two cannot be connected using integral multiples of the reciprocal lattice basis, and are as such classified into two different groups (K and K’), containing the points that can be reached using integral multiple of the basis vectors.

## Slide 10: Why graphene?
Unique electronic properties enabling novel devices beyond Transistors
  Photon-like behavior of charge carriers
CVD growth allows wafer-scale coverage
CMOS Compatible
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: These unique electronic properties of graphene make it very attractive when considering beyond-CMOS integration. In addition, the maturity and relative ease of fabrication wafer-scale graphene using CVD and its CMOS compatibility, make it a natural choice for wafer-scale beyond-CMOS integration.

## Slide 11: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: In what follows, we describe the use of graphene in a non-transistor-centric approach for different applications. We will present the use of graphene to build all-graphene neuromorphic or brain-like computers, discussing a new area-efficient architecture for brain-like computing that can be implemented using graphene.
We then preset the design of a low-loss diode using graphene, for the realization of mux-based logic families and low-loss energy scavenging elements. We show how the photon-like behavior of charge carriers in graphene can be harnessed to create asymmetrical conduction.
We then investigate the limits of scaling CVD graphene interconnects by studying the coupling between graphene ribbons operating in the diffusive-transport regime, showing that graphene interconnects are deeply scalable without.
We conclude by a discussion of the current technological limitations and information we have gathered when fabricating graphene devices, shedding light on some very interesting properties of graphene.

## Slide 12: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 13: Neuromorphic computing using CNNs
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Neural Networks have been very successful in classification and image processing problems
One circuit-friendly implementation (Cellular Neural Networks) have been around since the 1980s
CMOS CNN implementation are size limited
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 14: Cellular Neural Networks - Architecture
4x4 CNN
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 15: Cellular Neural Networks – System Model
We have 3 parameters in a CNN: Input (): External Stimulus State (): Internal State Output (): Function of the State
The network is stable as long as the output is related to the state by a monotonic, bound function (sigmoid)
Synaptic weights control circuit function and are determined offline
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 16: Cellular Neural Networks – Neuron Circuit Model
L. O. Chua and L. Yang, “Cellular neural networks: theory,” IEEE Trans. Circuits Syst., vol. 35, no. 10, pp. 1257–1272, 1988.
Input
Stimulus
State Variable
Output Sigmoid
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Canonical CNN implementations is suitable for CMOS
  Several Analog implementations available
  Nonlinearity not a problem as long as its monotonic
Synaptic weights implemented using transconductors
  Need to be tunable with good matching
  Sets a lower bound on the current consumption ()
  Number of Synapses >> Number of Neurons
Neuron RC controls system dynamics and speed
  Neuron C >> Parasitic Capacitance for reliable operation
  R not too big to reduce the noise in the system, but
Canonical CNN implementations is suitable for CMOS
  Several Analog implementations available
  Nonlinearity not a problem as long as its monotonic
Synaptic weights implemented using transconductors
  Need to be tunable with good matching
  Sets a lower bound on the current consumption (𝑔_𝑚∝𝐼)
  Number of Synapses >> Number of Neurons
Neuron RC controls system dynamics and speed
  Neuron C >> Parasitic Capacitance for reliable operation
  R not too big to reduce the noise in the system, but 𝑃∝1/𝑅

## Slide 17: Problems of CMOS CNN
Power Consumption
Dominated by Synapse Transconductors
Large number of Synapses
Matching and Tuning Requirements
Synapse Transconductance needs to be tunable
Synapses must be well matched
Speed Limitations
Neuron C >> Parasitics for Robustness
Lower RC means more power consumption
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 18: What can graphene do?
Graphene provides variable, finite channel resistance
  Voltage controlled resistor or low output resistance transistor
CVD graphene allow us to create a large number of devices
Graphene is compatible with CMOS
  Allows leveraging the high memory density available in CMOS
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 19: Graphene Resistance vs Gate Voltage
CVD graphene operates typically in the diffusive regime (Drude Model)
One popular model is the constant mobility model
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 20: All-Graphene CNN - Architecture
Fixed total R >>
M. Darwish, V. Calayir, L. Pileggi, and J. A. Weldon, “Ultracompact Graphene Multigate Variable Resistor for Neuromorphic Computing,” IEEE Trans. Nanotechnol., vol. 15, no. 2, pp. 318–327, Mar. 2016.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Neurons formed by a string of two voltage controlled resistors
  Inhibitory/Excitatory resistors pull towards ground/supply respectively
Neuron Capacitor stores the state
Synapses formed via two complementary digitally-controlled resistors
  Scales the output of the neuron before applying it to the inhibitory/excitatory control of the neighbor neuron
Both neurons and synapses formed via dual-gates graphene FETs

## Slide 21: All-Graphene CNN – Architecture Properties
Pros
Implicit sigmoidal behavior.
Synapse power consumption can be made arbitrarily small.
Reduced parasitic capacitance at state variable node.
Synapse matching required locally not globally.
Cons
Neuron RC limits speed.
More complicated training.
Network size limited by gate strength.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 22: Constant Mobility Model
(Charge-Neutrality Point)
: Contact Resistance
: Back gate oxide areal capacitance
: Electronic charge
: Number of squares in the channel
S. Kim, J. Nah, I. Jo, D. Shahrjerdi, L. Colombo, Z. Yao, E. Tutuc, and S. K. Banerjee, “Realization of a high mobility dual-gated graphene field-effect transistor with Al2O3 dielectric,” Appl. Phys. Lett., vol. 94, no. 6, p. 62107, 2009.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 23: Neuron/Synapse: Device Structure
M. Darwish, V. Calayir, L. Pileggi, and J. A. Weldon, “Ultracompact Graphene Multigate Variable Resistor for Neuromorphic Computing,” IEEE Trans. Nanotechnol., vol. 15, no. 2, pp. 318–327, Mar. 2016.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Back gate used to bias the device and top gates used to change the resistance.

## Slide 24: Notable Fabrication Details
Contacts cannot be sputtered to prevent damage to graphene
  Evaporation causes no kinetic impact damage unlike sputtering
Top gate oxide require a seed as non-functionalized ALD precursors do not react with the graphene surface and preferentially react with reactive graphene edges
Top gate oxide ALD relieves stress developed during contacting, etching and seed layer deposition (more on this later)
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 25: Neuron/Synapse: How they look like
3-bit Synapse
3-input Neuron
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 26: Interesting Synapse Behavior
VBG>VD
VBG<VD
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 27: Synapse as Dual-Slope Digital-to-Resistance Converter
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 28: Measured Synapse Resistance Change
Expected
Measured
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 29: Synapses as Digital-to-Resistance Converter
Synapses act as Digital-to-Resistance Converter
Slope and magnitude of resistance change controlled by back gate voltage
Process variability reduced using CMOS-like techniques (ex. Common centroid)
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 30: System-Level VerilogA Simulation
VerilogA models developed based on measurement results
Classification trained using Hebbian learning offline and successful up to 28% distortion
System can also perform edge and line detection
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 31: Conclusion
System-Circuit-Device co-design enable multi-level innovations
New architecture relaxes chip-level matching constraints
Graphene enables area-efficient implementation of synapses and neurons
Graphene synapses are compact digital-to-resistance converters
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 32: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 33: A review of graphene diodes
Linear dispersion and continuum of states except at the Dirac point make graphene diodes attractive
  Lossless as there is no potential barrier across PN junctions
  Relies on optics-inspired techniques for conduction anisotropy
Can be used for low-loss scavenging of RF power or diode-based mux logic
  Graphene MUX via two controlled back-to-back diodes
Characterized via the asymmetry [A = I(VFWD)/I(VBWD)]
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 34: Geometric Graphene Diodes
Geometric diodes proposed to achieve asymmetric conduction by collimation of charge carriers in one direction and not the other
Fabricated using exfoliated and CVD graphene
  Exfoliated graphene devices always had higher asymmetry
  Hints to the role of scattering
Maximum achieved asymmetry was ~1.37 using exfoliated graphene
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
D. Dragoman and M. Dragoman, “Geometrically induced rectification in two-dimensional ballistic nanodevices,” J. Phys. D. Appl. Phys., vol. 46, no. 5, p. 55306, Feb. 2013.

## Slide 35: Principle of operation of geometric diodes
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
D. Dragoman and M. Dragoman, “Geometrically induced rectification in two-dimensional ballistic nanodevices,” J. Phys. D. Appl. Phys., vol. 46, no. 5, p. 55306, Feb. 2013.

## Slide 36: Oblique Incidence Graphene Diodes
Graphene charge carriers follow a Snell’s-law like relation at interfaces
Total internal reflection of charge carriers at oblique interfaces if angles, doping and Fermi level set correctly
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 37: Proposed Oblique Incidence diode
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Define the angle

## Slide 38: Interface Transmission Asymmetry
Left-to-Right
Right-to-Right
E1 = 0.5 eV, E2 =-0.5eV
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 39: Oblique PN junction model
Scattering smears the angular distribution and limits the backward-to-forward resistance ratio
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 40: Measurement Results
A = RBWD/RFWD)
Highest Graphene Diode Asymmetry reported to date!
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Whiskers are standard deviation and point is the mean

## Slide 41: Conclusion
Geometric diodes show that exfoliated graphene is better than CVD graphene
Measurements show that CVD oblique incidence diodes outperform exfoliated geometric diodes
Asymmetry is still too low for practical devices
  Scattering and lead resistance need to be reduced
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 42: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 43: Graphene Coupler
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 44: Why study resistive coupling?
Ballistic-transport devices predicted to have periodic coupling coefficient like their optics counterparts
Diffusive-transport couplers never studied
  Could they be useful?
  How does diffusive transport affect the coupling coefficient?
Capacitive coupling and cross-talk have been thoroughly investigated, but no study of scaling limits in terms of resistive coupling
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 45: Electrical model of diffusive coupler
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Loss of phase information by scattering allows us to model coupling using a resistance
Sheet resistance of each branch assumed to be the same for simplicity
  Process gradient can be assumed negligible if ribbons are not too far apart
  Charge-puddles average out macroscopically
Coupling conductance per unit length obtained via Bardeen Transfer Hamiltonian (BTH)

## Slide 46: Is this model accurate?
Loss of phase information preserved
All distributed resistances should be random variables
Can be relaxed to first order models and when ribbon spacing is too wide relative to LER
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 47: SPICE simulation results
,
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
R1=R2

## Slide 48: Coupling conductance estimation
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Angular spread of transmission coefficient is low

## Slide 49: Coupling conductance results
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 50: Conclusion
Diffusive-transport couplers have an asymptotic coupling coefficient
  Not periodic like ballistic-transport couplers
Resistive coupling not a concern for deeply scaled graphene ribbons
Coupling conductance is negligible for ligthographically-defined ribbons
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 51: Outline
All-Graphene Neuromorphic Computing
Low-loss Graphene Diodes
Current Coupling in Diffusive-Transport Graphene
Current Technological Limitations
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 52: Impact of Metal-Graphene Interface on Device Performance
Joule heating increases channel temperature increasing scattering and reducing mobility
Proper device design enhances graphene-metal thermal contact allowing heat to escape through the contact reducing the channel heating
Thermal contact optimization should not affect electrical contact resistance to prevent reduction in electrical device performance
D. Saha, X. Yu, M. Darwish, M. Jeong, J. Freedman, A. Gellman, J. Weldon and J. Malen, “Developing Superior Alloy Contacts Optimized for Electrical and Thermal Transport at Metal-Graphene Interfaces”, MRS Spring, April 2017
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 53: Contact Metal Choice
Ni and Pd span the interaction spectrum with graphene from NiC formation to weak interaction with Pd
Compositionally Spread Alloy Film (CSAF) or Ni-Pd was evaporated on a blanket graphene film over 90 thermal SiO2 and graphene-metal interface thermal conductance (GTH) was evaluated FDTR (Frequency Domain Thermal Reflectance)
  All sample covered with Au transducer layer
Higher thermal interface conductance is desirable as it means more heat can flow across the metal contact rather than through the channel
D. Saha, X. Yu, M. Darwish, M. Jeong, J. Freedman, A. Gellman, J. Weldon and J. Malen, “Developing Superior Alloy Contacts Optimized for Electrical and Thermal Transport at Metal-Graphene Interfaces”, MRS Spring, April 2017
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 54: FDTR setup
J. Epstein, W. L. Ong, C. J. Bettinger, and J. A. Malen, “Temperature Dependent Thermal Conductivity and Thermal Interface Resistance of Pentacene Thin Films with Varying Morphology,” ACS Appl. Mater. Interfaces, vol. 8, no. 29, pp. 19168–19174, 2016.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Pump changes temperature
Probe measures changes in reflectance due to heating, which modulates its CW signal
Phase variation vs frequency fitted to obtain surface conductance after fitting to multi-layer heat transfer model

## Slide 55: Evaluated Metal-Graphene GTH
D. Saha, X. Yu, M. Darwish, M. Jeong, J. Freedman, A. Gellman, J. Weldon and J. Malen, “Developing Superior Alloy Contacts Optimized for Electrical and Thermal Transport at Metal-Graphene Interfaces”, MRS Spring, April 2017
Elemental metals lie in this range
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Ni-Pd allow with ~10% Pd gives very large increase thermal interface conductance  More heat flows through the contact rather than chanel

## Slide 56: Electrical Measurements
Currently another CSAF sample is being created with electrical and thermal measurements structures
  Electrical: Linear TLM, Circular TLM, CBKR and 4-point probe
  Thermal: Metal strips
Will the electrical contact resistance show the same trend?
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Linear Transfer Length Method
Circular Transmission Line Method

## Slide 57: Stress in GFETs
Contacts anchor the graphene to the substrate
Graphene is single-atom thick, surrounded by materials of different thermal expansion coefficient
  Highly prone to stress
α1
Top Gate Oxide
Silicon Substrate
Bottom Gate Oxide
Graphene
Contact
Contact
Adhesion
Adhesion
α2
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 58: Probing Stress in Graphene
2D Raman peak red shifts under tension
2D Peak FWHM function of both stress and charge fluctuations
2D peak splits under
  Function of orientation, polarization and strain magnitude
Tension
M. Mohr, J. Maultzsch, and C. Thomsen, “Splitting of the Raman 2D band of graphene subjected to strain,” Phys. Rev. B, vol. 82, no. 20, p. 201409, Nov. 2010.
Compression
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Left/Right on the scale is more intuitive in the discussion over graphs.
Mention the 2D shift being an overtone of the breathing mode increasing the wavelength and hence causing red shift

## Slide 59: Device Structure used in Strain Evaluation
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 60: Strain Evolution during GFET Fabrication
M. Darwish, D. Saha, J. Malen, and J. A. Weldon, “Processing-Induced Strain in Dual-Gated Graphene FETs”, in IEEE Nano, 2017.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Single point left
Scan data right
ALD seems to anneal effect of stress by seed layer.

## Slide 61: Impact of Developer Chemistry on Device Performance
Photoresist developer chemistry can contain Metal-Ion Containing (MIC) or be Metal-Ion Free (MIF)
Choice of developer chemistry is dictated by process compatibility and developer properties
Impact MIF and MIC developers on device performance evaluated using the constant mobility model
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 62: Dirac Point Shift
MIC
N=25
MIC
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: The results for each developer are presented using box plots, Central marker for median, Box edges are 25 and 75 percentile edges, Whiskers extend to most extreme data points.
Hysteresis due to trapped interface charges screened by metla charges

## Slide 63: Field-Effect Mobility and Charged-Impurity Concentration
MIC
N=25
MIC
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: The results for each developer are presented using box plots, Central marker for median, Box edges are 25 and 75 percentile edges, Whiskers extend to most extreme data points.

## Slide 64: Contact Resistance
MIC
N=25
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Large spread tells us about repeatability and interface quality

## Slide 65: Mobility and Charged-Impurity Concentration
The mobility and charged-impurity concentration are inversely proportional
The relation between and is given as:
The value of the proportionality constant has been evaluated theoretically to be
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 66: Mobility vs Charged-Impurity Concentration
M. Darwish, D. Saha, J. Malen, and J. A. Weldon, “A Comparison of the Impact of Metal - Ion Containing and Metal - Ion Free Photoresist Developers on Graphene Field - Effect Transistors,” in IEEE Nano, 2017.
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Mobility worst than predicted theoretically

## Slide 67: Residual Photoresist on Graphene Channel
Notes: Large residual in AZ Dev and AZ400K. Metal-Graphene interface certainly less resist, but confirms our prediction of the interface quality.

## Slide 68: Conclusion
Metal-Graphene electrical and thermal interface co-optimization can be rapidly evaluated using CSAF films
  Ni-Pd films very promising
MIC developers degrade mobility due to charged-impurity scattering increase, but reduce interface-trapped charge hysteresis
Mobility degradation due to charged-impurity scattering is worse than theoretically predicted
Some resists leave considerable residual over graphene, causing large spread in reported contact resistance and interface-dependent phenomena

## Slide 69: What’s next?
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 70: Future Work – Contact Engineering
Co-optimization of electrical and thermal interface contact resistance by alloying
  CSAF films allow rapid evaluation and fine-tuning of contact alloys
Impact of adhesion layer evaluated using partial-coverage films
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 71: Future Work – Graphene leads for 2D materials
2D materials are doped by contacts
Integration of different metals for different device doping type is limiting, if possible
Graphene can act as an intermediate lead between the metal and 2D semiconductor to alleviate contact doping
  Can be combined with alloyed metal-graphene contacts
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work
Notes: Graphene gets doped – doesn’t matter due to e-h symmetry but screens 2D semiconducting channel from doping

## Slide 72: Future Work – Oblique diodes using hBN/G/hBN heterostructure
Exfoliated graphene between hBN flakes has low scattering
  Mean free paths (MFP) for up to a micron at room temperature
Oblique-incidence diodes fabricated using hBN/G/hBN heterostructure will have reduced scattering and higher asymmetry
The use of edge contacts allows reducing the parasitic contact resistance considerably
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 73: Future Work – CVD hBN with CVD graphene
hBN is the optimal substrate for graphene
Combining CVD hBN with CVD graphene enables wafer-level integration of high performance graphene devices
CVD of hBN has been demonstrated, but transfer along with CVD graphene is yet to be explored
Introduction
Graphene CNN
Low-loss Diode
Diffusive Coupler
Tech. Limitations
Future Work

## Slide 74: Acknowledgements (1)
Prof. Jeffrey A. Weldon.
Prof. Larry Pileggi
Prof. Randall Feenstra
Prof. Eric Pop (Stanford University)

## Slide 75: Acknowledgements (1)
Prof. Andrew Gellman
Prof. Jonathan Malen
Prof. Ben Hunt
Prof. Tzahi Cohen-Karni

## Slide 76: Acknowledgments (2)
Dr. Mohamed Abdelmoula
Dr. Doron Naveh
Dr. Mathew Moneck
Nanofab Staff: Mark Weiler, Norman Gottron, Mason Risley, James Rosvanis
Ex. Nanofab Staff: Carsen Kline and Chris Bowman

## Slide 77: Acknowledgments (3)
Prof. Jelena Kovačević
Dipanjan Saha
Ning Wang (Stanford University)
Dr. Sergio de la Barrera
Devashish Goplan
Xiaoxiao Yu

## Slide 78: Acknowledgments (4)
David Bromberg, Tom Jackson, Jeff Zayas, Sean Yen, Omer Ozdemir, Yunlu Li, Isen Ozalp, Yunus Kesim, Sungho Kim, Nail Etkin “LL” Can Akkaya, Burac Erbagci, Luca Colombo, Mats Forssell, MaryBeth Galanko, Ashwati Krishnan, Metin Guney, Andrew Ong, Cheng-Ming Chow, Ekin Sumbul, Ahmed Abdelgawad, Usama Zaghloul, Ahmed Khairi, Ahmed Hussein, Mazen Soliman, Mohamed Mahmoud, Khaled El-Galaind, Ahmed Hefny and Waleed Ammar
Dr. Amani Attia
Dr. Ashraf Taha
This work was supported in part by Systems on Nanoscale Information fabriCs (SONIC), one of the six SRC STARnet Centers, sponsored by MARCO and DARPA

## Slide 79: Acknowledgments (5)
My Father, Omar Abdulaziz
My Mother, Mariam
My Sister, Mennatullah
My Son, Bilal
My Wife and support, Mai

## Slide 80: Questions?

## Slide 81: Fabrication Steps (1): Contact photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Positive photoresist (S1805) and lift-off layer (LOR3A) spin and bake
(b) Exposure and development in CD26 (TMAH-based MIF developer prevents graphene doping)

## Slide 82: Fabrication Steps (1): Contact photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties

## Slide 83: Fabrication Steps (2): Contact deposition and lift-off
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Evaporation of contact metal stack (Ti/Pd 1.5/40 nm at a rate < 0.3 Å/sec)
(b) Lift-off in a dedicated Microposit 1165 remover at 70 °C to prevent contamination

## Slide 84: Fabrication Steps (2): Contact deposition and lift-off
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties

## Slide 85: Fabrication Steps (3): Channel Etch Mask Photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Positive photoresist (S1805) and lift-off layer (LOR3A) spin and bake
(b) Exposure and development in CD26 (TMAH-based MIF developer prevents graphene doping)

## Slide 86: Fabrication Steps (4): Channel Definition using RIE
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Etch the exposed graphene in O2 plasma (20 W for 1 minute at 10 mTorr)
(b) Etch mask removal in a dedicated Microposit 1165 remover at 70 °C to prevent contamination

## Slide 87: Fabrication Steps (3): Channel Etch Mask Photolithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties

## Slide 88: Fabrication Steps (5): Top oxide seed layer and oxide deposition
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Evaporation of 1.5 nm of Al to act as a seed layer for ALD as non-functionalized ALD reacts only with graphene edges. 1.5 nm of Al are fully oxidized in air (Native Al oxide is 2.5 nm thick)
(b) ALD of Al2O3 at 150 °C to finish the top gate oxide deposition

## Slide 89: Fabrication Steps (6): Top gate e-beam lithography
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Positive e-beam resist (PMMA A7) and spin and bake beyond glass transition temperature
(b) Exposure and development (1:3 MIBK:IPA developer) of top gate electrodes

## Slide 90: Fabrication Steps (7): Top gate deposition
Beyond-CMOS
Graphene CNN
RG Mux Logic
Graphene Properties
(a) Evaporation of top gate metal
(b) Lift-off of top gate metal in a dedicated acetone bath

## Slide 91: Fabrication Steps (7): Top gate deposition